## Slide 1: Regenerative solutions
creos™ xenografts

## Slide 2: creos™ biomaterials A comprehensive portfolio for soft tissue & bone regeneration
Bone Graft Substitutes
creos™ xenogain
Soft Tissue Matrix
creos™ mucogain
Membranes
creos™ xenoprotect

## Slide 3
A membrane with outstanding handling that facilitates bone gain
creos™ xenoprotect

## Slide 4: Einfache Handhabung
4. Facilitates bone gain
  Good clinical results.
  Excellent tissue compatibility.
2. High mechanical strength
Excellent suture retention.
Highly tear-resistant, making it easy to suture or fixate with pins.
1. Outstanding handling
  Does not stick to instruments.
  Repositioning in-situ possible.
  Minimal size increase when hydrated.
3. Enduring resistance to degradation in vivo
  Manufacturing process intended to preserve the natural structure of the collagen fiber network, to confer a high resistance to degradation.

## Slide 5
creos™ xenoprotect is a membrane composed of a network of highly purified porcine collagen and elastin fibers.
The manufacturing process is intended to preserve the natural structure of the collagen fiber network, to confer a high resistance to degradation.
A natural barrier with outstanding handling properties.
What is creos™ xenoprotect?

## Slide 6
Available in 3 sizes
Article | Size
N1520 | 15x20 mm
N2530 | 25x30 mm
N3040 | 30x40 mm

## Slide 7
1. Outstanding handling
Both sides can face the defect
Easy to trim (dry or wet)
Low surface expansion when hydrated
Does not stick to instruments
  Both sides can face the defect
  Easy to trim (dry or wet)
  Low surface expansion when hydrated.
  Does not stick to instruments, repositioning in-situ possible.

## Slide 8
2. High mechanical strength and tear resistance#
Gasser A, Wessing B, Eummelen L, et al. Mechanical stability of collagen membranes: an in vitro study. J Dent Res 2016;95(Spec Iss A): 1683
# as shown in an in vitro study
* statistically significant

## Slide 9
2. High suture resistance#
Gasser A, Wessing B, Eummelen L, et al. Mechanical stability of collagen membranes: an in vitro study. J Dent Res 2016;95(Spec Iss A): 1683
# as shown in an in vitro study
* statistically significant

## Slide 10
3. Enduring resistance to degradation
Slower in vitro bio-degradation compared to another chemically non-crosslinked barrier membrane.
Bozkurt A, Apel C, Sellhaus B, et al. Differences in degradation behavior of two non-cross-linked collagen barrier membranes: an in vitro and in vivo study. Clin Oral Implants Res 2014; 25(12):1403-1411
creos™ xenoprotect
reference membrane
creos™ xenoprotect features an almost twofold lower degradation rate compared to a reference chemically non-crosslinked membrane when exposed to natural enzymes in vitro.
* statistically significant
*

## Slide 11
3. Enduring resistance to degradation #
Bozkurt A, Apel C, Sellhaus B, et al. Differences in degradation behavior of two non-cross-linked collagen barrier membranes: an in vitro and in vivo study. Clin Oral Implants Res 2014; 25(12):1403-1411
Initial thickness
creos™ xenoprotect
Initial thickness
reference membrane
Histology 20 weeks
after implantation
After 20 weeks, the thickness of creos™ xenoprotect decreased only slightly, whereas the reference membrane showed a thickness loss of around 50%, confirming the higher stability of creos™ xenoprotect against biodegradation in vivo.
# as shown in an animal model (rat, subcutaneous)
* statistically significant
1000
800
600
400
200
0
Initial thickness
creos™ xenoprotect
Initial thickness
reference membrane
creos™ xenoprotect
reference membrane
Membrane thickness [µm]
20 weeks after implantation
*
creos™ xenoprotect
reference membrane

## Slide 12
4. creos™ xenoprotect facilitates bone gain #
Omar O, Dahlin A, Gasser A, et al. Tissue dynamics and regenerative outcome in two resorbable non-cross-linked collagen membranes for guided bone regeneration: A preclinical molecular and histological study in vivo. Clin Oral Implants Res 2018;29(1):7–19.
Bone defect
Bovine bone grafts
creos™ xenoprotect
or
reference membrane
creos™ xenoprotect demonstrated significantly higher new bone formation in the central portion of the defect compare to the reference membrane.
# as shown in an animal model (rat)
* statistically significant

## Slide 13
4. Good clinical results in the treatment of dehiscence defects
Wessing B, Emmerich M, Bozkurt A. Horizontal ridge augmentation with a novel resorbable collagen membrane: a retrospective analysis of 36 consecutive patients. Int J Periodontics Restorative Dent 2016;36(2):179–187.
Of the 49 included patients, 24 were treated with creos™ xenoprotect and 25 with a reference membrane.
For creos™ xenoprotect, the mean defect height at implant insertion was 5.1 ± 2.1 mm and reduced at reentry by 81%.
Defect at implant insertion
Defect at re-entry (6 months)
reference membrane
creos™ xenoprotect

## Slide 14
Why creos™ xenoprotect?
1. Outstanding handling
Low surface expansion when hydrated.
Easy to trim (dry or wet) and does not stick to instruments.
Repositioning in-situ possible.
Both sides can face the defect.
2. High mechanical strength
Excellent suture retention.
Highly tear-resistant, making it easy to suture or fixate with pins.
3. Enduring resistance to degradation in vivo
Manufacturing process intended to preserve the natural structure of the collagen fiber network, to confer a high resistance to degradation.
4. Facilitates bone gain
  Good clinical results.
  Excellent tissue compatibility in vivo.

## Slide 15: More scientific evidence is to be found in the following publications
Key scientific evidence, creos™ xenoprotect:
Gasser A, Wessing B, Eummelen L, et al. Mechanical stability of collagen membranes: an in vitro study. J Dent Res 2016;95(Spec Iss A): 1683
Bozkurt A, Apel C, Sellhaus B, et al. Differences in degradation behavior of two non-cross-linked collagen barrier membranes: an in vitro and in vivo study. Clin Oral Implants Res 2014; 25(12):1403-1411
Omar O, Dahlin A, Gasser A, et al. Tissue dynamics and regenerative outcome in two resorbable non-cross-linked collagen membranes for guided bone regeneration: A preclinical molecular and histological study in vivo. Clin Oral Implants Res 2018;29(1):7–19.
Wessing B, Emmerich M, Bozkurt A. Horizontal ridge augmentation with a novel resorbable collagen membrane: a retrospective analysis of 36 consecutive patients. Int J Periodontics Restorative Dent 2016;36(2):179–187.

## Slide 16
Soft tissue regeneration made smarter.
creos™ mucogain
Unique oriented porous structure designed for guided soft tissue regeneration

## Slide 17
5 Clinically effective
  Shown to promote soft tissue health and maintain adequate soft tissue thickness in a clinical study. 2
4. Excellent handling
Easy to use.
High suture retention and stress resistance.
Memory effect after hydration and cycling loading in vitro.
Trim to precisely fit surgical site.
Substitutes the need for a second surgical site (often associated with pain and bleeding for the patient)
2. Patented method
  Oriented open porous matrix structure.
  Designed to promote soft tissue regeneration through the migration of cells and blood vessels into the matrix.
3. Variety of choice
  A choice of different sizes and thicknesses.
  Designed to replace autologous grafts in several indications. 1
1 See Instructions For Use for full prescribing information, including indications, contraindications, warnings and precautions.
2 Wessing B et al. Clinical Oral Implant Research 2019.

## Slide 18
creos™ mucogain is a matrix of highly purified porcine collagen and elastin.
creos™ mucogain features oriented open pores thanks to a patented manufacturing method.
The resulting matrix features mechanical strength, stress resistance and a memory effect.
What is xenogain?
What is creos™ mucogain?

## Slide 19
What is xenogain?
1. Substitutes the need for a second surgical site
No need for a second surgical site, which is associated with post-operative pain, bleeding, swelling and infection.1
1 Harris R.J 2005. Griffin T.J. et al.2006. Aguirre-Zorzano L.A. et.al 2017

## Slide 20
What is xenogain?
2. A patented manufacturing process
Directional solidification method followed by freeze-drying.

## Slide 21
What is xenogain?
3. A variety of choice
Article | Size | Thickness
MU15203 | 15x20 mm | 3 mm
MU25303 | 25x30 mm | 3 mm
MU15205 | 15x20 mm | 5 mm
MU25305 | 25x30 mm | 5 mm

## Slide 22
What is xenogain?
4. Memory effect
When hydrated, the initial volume of the graft is maintained after repeated compression
Damink O.L., Heschel I., Leemhuis H. et all. Soft tissue volume augmentation in the oral cavity with a collagen-based 3D matrix with orientated open pore structure. Current Directions in Biomedical Engineering 2018; 4(1): 237 – 241
Chart: 
| 0 | 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8 | 8.5 | 9 | 9.5 | 10 | 10.5 | 11 | 11.5 | 12
 | 100 | 28.6432 | 99.4975 | 29.1457 | 99.4975 | 29.1457 | 100 | 29.1457 | 98.995 | 29.1457 | 98.995 | 28.6432 | 97.9899 | 28.6432 | 98.4925 | 29.1457 | 97.9899 | 27.1357 | 98.4925 | 28.6432 | 98.995 | 28.6432 | 98.4925 | 29.1457 | 98.4925
 | 100 | 28.6432 | 99.4975 | 29.1457 | 99.4975 | 29.1457 | 100 | 29.1457 | 98.995 | 29.1457 | 98.995 | 28.6432 | 97.9899 | 28.6432 | 98.4925 | 29.1457 | 97.9899 | 27.1357 | 98.4925 | 28.6432 | 98.995
50
creos™ mucogain thickness [% of initial size]

## Slide 23
Tissue integration and formation of new blood vessels due to the tube-like channel structure.
The matrix is replaced by newly formed autogenous soft tissue in vivo.
Damink O.L., Heschel I., Leemhuis H. et all. Soft tissue volume augmentation in the oral cavity with a collagen-based 3D matrix with orientated open pore structure. Current Directions in Biomedical Engineering 2018; 4(1): 237 – 241
5. Designed to promote soft tissue regeneration through the migration of cells and blood vessels into the matrix.

## Slide 24
What is xenogain?
5. Clinically effective
creos™ mucogain shown to promote soft tissue health and maintain adequate soft tissue thickness.#
In 45 patients, a follow-up of up to 4.5 years (mean of 1.8 ± 1.3 years) demonstrated that creos™ mucogain promotes soft tissue health and maintains adequate soft tissue thickness.
Wessing B, Boekema B and Gonzalez-Martin. Soft tissue augmentation with a collagen-based 3D matrix with directed pore channels. Clinical Oral Implant Research 2019:Volume30, IssueS19.
Initial situation
8 months post-treatment
Cirillo I, Encalada C, Periodontal plastic surgery: treatment of multiple gingival recessions. FOR.org
# as shown in a clinical study:
Wessing B et al. Clinical Oral Implant Research 2019

## Slide 25
1. No need for a second surgical site
  A second surgical site is associated with post-operative pain, bleeding, swelling and infection.1
2. Patented method
  Oriented pore structure
  Migration of cells into the matrix
3. Variety of choice
  Two thicknesses (3 & 5 mm)
4. Excellent handling
  Easy to use
  Memory effect, mechanical strength
5. Clinically effective
  Shown to promote soft tissue health and maintain adequate soft tissue thickness in a clinical study.2
Why creos™ mucogain ?
1 Harris R.J 2005. Griffin T.J. et al.2006. Aguirre-Zorzano L.A. et.al 2017.
2 Wessing B et al.. Clinical Oral Implant Research 2019.

## Slide 26: More scientific evidence is to be found in the following publications
Key scientific evidence, creos™ xenogain:
Boekema B., Vlig F, Damink O.L. et al. Effect of pore size and cross-linking of a novel collagen-elastin dermal substitute on wound healing. J Mater Sci Mater Med 2014:25(2):423-433
Wessing B, Boekema B and Gonzalez-Martin. Soft tissue augmentation with a collagen-based 3D matrix with directed pore channels. Clinical Oral Implant Research 2019:Volume30, IssueS19.
Wessing B, Vasilic N. Soft tissue augmentation with a new regenerative collagen 3-D matrix with oriented open pores as a potential alternative to autologous connective tissue grafts. Clin Oral Implants Res. 2014 Sep;25(s10)
Sanz-Martin I, Encalada C, Sam-Sanchez I, et al. Soft tissue augmentation at immediate implants using a novel xenogeneic collagen matrix in conjunction with immediate provisional restorations: A prospective case series. Clin Implant Dent Relat Res 2019;21(1):145-153.

## Slide 27
creos™
creos™

## Slide 28
GMT69057 © Nobel Biocare Services AG, 2020. All rights reserved. Distributed by: Nobel Biocare. Legal manufacturer for creos™ xenoprotect and creos™ mucogain is Matricel GmbH, Kaiserstrasse 100, D-52134 Herzogenrath, Germany.
Nobel Biocare, the Nobel Biocare logotype and all other trademarks are, if nothing else is stated or is evident from the context in a certain case, trademarks of Nobel Biocare. Please refer to nobelbiocare.com/trademarks for more information.
Product images are not necessarily to scale. All product images are for illustration purposes only and may not be an exact representation of the product.
Disclaimer: Some products may not be regulatory cleared/released for sale in all markets. Please contact the local Nobel Biocare sales office for current product assortment and availability.
For prescription use only. Caution: Federal (United States) law restricts this device to sale by or on the order of a licensed clinician, medical professional or physician. See Instructions For Use for full prescribing information, including indications, contraindications, warnings and precautions.